Note:

This document contains information and notes in hidden text.

If you need assistance to view & hide text, instructions are at this link:

http://www.marlite.com/hidden-notes-instructions.aspx

Delete this note and hyperlink after editing is complete.

The following specification has been developed by:

Marlite

202 Harger St.

Dover, Ohio

Tel: (330) 343-6621

Fax: (330) 343-4668

Email:  info@marlite.com

Website: www.marlite.com

to assist Architects and Designers in the specification of Marlite’s Flame Safe Panel Systems featuring 7/16” (1.11 cm) thick panels that are attached to finished sub-walls having appropriate support for installation of the product.  Marlite’s Flame Safe Panels are Class C and Class A construction 3-ply lamination with HPL faces on wood fiber substrate with a balancing backer.

Refer to separate Marlite Guide Specification Sections 09 7710 sections for other Marlite Framed Decorative Panel and Trim systems, Sections 06 2510 for Marlite prefinished panels, Section 09 7730 for Marlite decorative FRP panels, and Marlite Section 09 8430 for Acoustical Panels.

The section has been formatted in accordance with the principals embodied in the Construction Specifications  Institute's  Manual of Practice and is intended for use in conjunction with Contract Conditions, Bidding Conditions and General Requirements developed in accordance with CSI guidelines. Notes to the specifier are included. Options that must be selected by the specifier are shown in brackets [         ].   Inapplicable clauses shall be deleted.

SECTION 09 7710 – FRAMED DECORATIVE PANEL SYSTEMS

GENERAL

SUMMARY

Section Includes:   Decorative 7/16” (1.11 cm) thick prefinished panel mechanically and adhesively applied directly to a solid substrate, utilizing a pre-engineered application process.

Hardware:  Extruded aluminum joinery moldings, extruded aluminum perimeter trim moldings and mechanical fasteners.

Panels:

Fire-Rated HPL laminated to Fire-Rated wood fiber substrate, with balancing backer.

Non Fire-Rated HPL laminated to wood fiber substrate, with balancing backer.

Products Not Furnished or Installed under This Section:

Wood Veneer casework.

Gypsum Board backup.

RELATED SECTIONS

Section [____] - Wood [Metal] Stud Framing

Section [____] - Custom Cabinets

Section [____] - Solid Wood Paneling

Section [____] - Gypsum Wallboard.

Section [____] - Painting & Transparent Finishes.

Section [____] - Resilient Base.

REFERENCES

References are listed as a convenience and are often deleted in their entirety.  If required by the user agency delete references from the list below that are not actually required by the text of the edited section

American Society for Testing and Materials:  Standard Specifications (ASTM)

ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

Architectural Woodwork Standards as published by the Architectural Woodwork Institute, the Architectural Woodwork Manufacturers Association of Canada, and the Woodwork Institute.

Architectural Woodwork Standards - Edition 1.

SUBMITTALS

Product Data:  Submit sufficient manufacturer's data to indicate compliance with these specifications, including:

Preparation instructions and recommendations.

Storage and handling requirements and recommendations.

Installation methods.

Shop Drawings:  Submit elevations of each wall showing location of paneling and trim members with respect to all discontinuities in the wall elevation.

Selection Samples:  Submit manufacturer’s standard color and pattern selection samples representing manufacturer's full range of available colors and patterns pertinent to the project.

Samples for Verification:  Submit 6” (154mm) by 10” (254mm) section of panel for each panel selected indicating the color, texture, and pattern required.

Submit complete with specified applied finish.

Exposed Molding and Trim:  Include 4” (101mm) long samples of each type, finish, and color.

Manufacturers Material Safety Data Sheets (MSDS) for adhesives, sealants and other pertinent materials prior to their delivery to the site (available as downloads for most Marlite’s products at http://www.marlite.com/tech-details.aspx or by contacting Marlite at info@marlite.com).

Maintenance Instructions

QUALITY ASSURANCE

ASTM E 84 Definition: Strict interpretation of the ASTM E 84 fire rating applies only to surface burning characteristics of a panel.  Marlite Connections Fire-Rated panels and trim are intended to provide a Class A Fire-Rated application, as defined by ASTM E 84 classification, but are not intended to be included in the creation of Fire-Rated demising wall construction.  ASTM E 84 fire rating for a Class A material requires a flame spread 25 or less, along with a smoke development maximum of 450.  ASTM E-84 fire rating for a Class C material requires a flame spread of between 26 and 200, along with a smoke development maximum of 450.

As all current U.S. building fire rating codes are pertinent only to surface burning characteristics of applied materials, the balancing backer is not subject to scrutiny within fire ratings.

Conform to building code requirements for interior finish for smoke and flame spread requirements as tested in accordance with:

ASTM E 84 (Method of test for surface burning characteristics of building Materials)

Required Rating – Class [A] [C].

DELIVERY, STORAGE AND HANDLING

Deliver panels and associated materials factory packaged on strong pallets and properly packaged or protected.

Upon delivery carefully inspect all cartons, packages, pallets and protective wrap for damage or material shortage.

Open and inspect suspect packages, cartons or wrapped pallets for damage.

Contact shipper immediately to report any damaged or missing materials.

Contact Marlite @ (800) 377-1221 immediately to report any damaged or missing materials.

Contact Marlite @ (800) 377-1221 with any questions, problems or concerns.

Store products in manufacturer's unopened packaging until ready for installation.

Maintain plastic or other protective wrap in place during on site handling until ready for installation.

Keep panels clean and do not stack panels after removal of protection.

Store and dispose of solvent-based materials, and materials used with solvent-based materials, in accordance with requirements of local authorities having jurisdiction.

PROJECT CONDITIONS

Wood composite panels are subject to the effects of humidity and temperature.  Do not use in kitchens, rest rooms, or other high humidity areas.

Partition walls are to be finished and the building completely closed. Walls shall be thoroughly dry and concrete cured and dry before starting installation.

HVAC system must be operable and installation area must be balanced to normal operating conditions.

Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results.  To ensure product performance, a temperature range of 60°-80°F (16°C-27°C) and a humidity range of 35-55% must be maintained during storage, installation and product life cycle.  Do not install products under environmental conditions outside manufacturer's absolute limits.

COORDINATION AND SEQUENCING

Except as specified by the architect, it’s recommended to locate trim members so that panel lines coordinate with doors, headers, jambs and other discontinuities in a wall.

Vapor barrier shall be used on exterior walls behind backing to discourage warping.

Delete the following if panels are not used on casework

Coordinate with casework manufacturer.  Deliver material to the fabrication shop.

WARRANTY

For longer warranties contact Marlite.

Standard Warranty:  All products shall be warranted to be free from defects for a period of 30 days after installation.

PRODUCTS

ACCEPTABLE PRODUCT

        - Marlite;   202 Harger Street, Dover, OH  44622.  800-377-1221 FAX (330) 343-4668 Email:  info@marlite.com www.marlite.com.

Product:  Flame Safe Panel System, designated as CP-3, CP-4, CP-6 & CP-7

Specifier to select and delete unused.

CP-3 Divider System.  A progressive wall panel system featuring a one-piece hidden vertical divider molding that minimizes molding appearance.  Utilizing this system requires a 1/16” (1.6mm) space between panels to accommodate dimensional expansion and contraction.

CP-4 Divider System.  A non-progressive wall panel system featuring a two-piece hidden divider molding that allows for ease of panel installation or replacement.

CP-5 Divider System.  A progressive wall panel system featuring a one-piece hidden vertical divider molding similar to CP-3, but has an added protrusion in the reveal between panels for aesthetic effect.

CP-7 Divider System.  A non-progressive wall panel system featuring a one-piece hat channel shaped divider molding that allows for ease of panel installation or replacement.

The inside of the divider molding can be concealed with a matching or contrasting strip of decorative laminate (HPL).

An aluminum insert is also available to conceal the system attachment screws and lower portion of the divider molding.

HARDWARE

Hardware and Trim Material:   Heavy weight extruded aluminum 6063-T5 alloy furnished in lengths as indicated and factory prefinished.

Provide the following exposed edge trim, trim receivers, trim profiles and other manufacturer’s standard members as required for a complete installation.

Specifier to select lengths and profiles as required by the design and delete unused.

Horizontal Cap Molding – Marlite part #CP-107 Edge Cap.  Available in 8’ (2.44m) and 10’ (3.05m) lengths.

Vertical Cap Molding – Marlite part #CP-280 Edge/Inside Corner. Available in 8’ (2.44m) and 10’ (3.05m) lengths.

90 Degree Outside Corner – Marlite part #CP90C Outside Corner. Available in 8’ (2.44m) and 10’ (3.05m) lengths.

135 Degree Outside Corner – Marlite part #CP135C Outside Corner. Available in 8’ (2.44m) and 10’ (3.05m) lengths.

Aluminum Finishes:

Concealed

Mill finish

Exposed

Specifier to select and delete unused.

Clear Satin Anodize

Black Satin Anodize

PANELS

Panels shall be Flame Safe Panel System with Class C or Class A construction and finish as follows.

Specifier to select and delete unused.

High Pressure Laminate.

Vertical grade decorative laminate face over wood fiber substrate, with balancing backer.

Wilsonart Laminate

Type 602 - .032” (.85mm) Fire-Rated decorative face

Type 264 - .030” (.76mm) Fire-Rated balancing backer

Type 335 - .030” (.76mm) Non Fire-Rated decorative face

Type 235 - .028” (.71mm) Non Fire-Rated balancing backer

Formica Laminate

Type 32 - .032” (.85mm) Fire-Rated decorative face

Type 87 - .028” (.71mm) Fire-Rated balancing backer

Type 20 - .030” (.76mm) Non Fire-Rated decorative face

Type 9302 - .025” (.63mm) Non Fire-Rated balancing backer

Nevamar

Type VR-3 - .032” (.85mm) Fire-Rated decorative face

Type VF-3 - .028” (.71mm) Fire-Rated balancing backer

Other than listed laminate manufacturers.

Consult directly with Marlite.

Colors

Fire-Rated

All solid colors and most wood-grain patterns are available from most manufacturers.

Non Fire-Rated

All colors and patterns are available from most manufacturers.

Not all patterns and wood-grain colorways are manufactured as Fire-Rated.  When available, certain restrictions can apply for specialty finishes on Fire-Rated laminates.  Availability can be checked through Marlite or by contacting the laminate manufacturer directly.

Finishes

Fire-Rated

All standard surface finishes and most specialty surface finishes are available from most manufacturers.

Non Fire-Rated

All standard surface finishes are available from most manufacturers.

Not all surface finishes are manufactured as Fire-Rated.  When available, certain restrictions can apply for specialty surface finishes on Fire-Rated laminates.  Availability can be checked through Marlite or by contacting the laminate manufacturer directly.

Grain Direction

Manufacturer’s standard (typically parallel with longest dimension of HPL product).

Panel Size

Nominal 24” wide x 96” long.

Nominal 48” wide x 96” long.

Nominal 24” wide x 120” long.

Nominal 24” wide x 120” long.

Wood Fiber Substrate.

Specifier to select and delete unused.

Class A

Marlite panels are typically manufactured using various wood fiber substrates having either 75%, 82% or 100 % recycled wood waste.   When available as Fire-Rated, a higher percentage may be specified if required for environmental credits.

Class C

Marlite panels are typically manufactured using various wood fiber substrates having either 75%, 82% or 100 % recycled wood waste.   When available as Fire-Rated, a higher percentage may be specified if required for environmental credits.

FABRICATION

All framing, panels, hardware and accessories shall be factory finished and ready to install except for field fabrication as required by jobsite and perimeter conditions.

Refinish field cut panel edges in accordance with manufacturer’s instruction before installation.

For all cut-outs, drill corners for a minimum 1/8” radius.

EXECUTION

EXAMINATION

Installer's Examination:  Examine conditions under which construction activities of this section are to be performed.  Submit written notification to Architect and system manufacturer if such conditions are unacceptable.  Beginning erection constitutes installer's acceptance of conditions.

Verify that a vapor barrier has been provided on exterior walls behind backing to prevent warping.

Verify backing and mounting surfaces are smooth, solid, and flat.  [All drywall joints are to be taped and finished].

Verify that walls are sealed, primed before installation begins.

Verify mechanical, electrical, and building service and/or items affecting work of this section are placed and ready to receive this work.

Verify that structural stud spacing does not exceed 24” on-center.

Structural walls are to be finished, with building completely closed.   Walls shall be thoroughly dry before starting installation.

PREPARATION

Conditioning:  Panels must be allowed to acclimate to a balanced environment in the installation location for 72 hours prior to installation.

Protect existing surfaces with drop cloths.

Except as directed by the architectural drawings, before installing, examine panels and arrange to achieve best combination of color, pattern, texture and grain.

INSTALLATION

Install all materials in strict accordance with the manufacturer’s installation instructions and recommendations, with hardware straight, plumb, and level.

Anchor units rigidly and securely in place.

Cut sheets to meet existing supports.

Fasten supports and trim using appropriate fasteners into a stud or other solid substrate at centers as specified by the manufacturer.  Where screws do not hit the studs, fasten with adhesive in accordance with the manufacturer’s recommendations.  Pre-drill holes thru the members and fasten the screw flush with the flange on the aluminum profile. Where necessary countersink for the screw head to seat flush with the flange.

Avoid contamination of the panel faces with adhesives, solvents or cleaners during installation.

CLEANING AND PROTECTION

Clean and remove dust and other foreign matter from panel and framing surfaces.  Clean finishes in accordance with manufacturer's instructions.

END OF SECTION 09 7710