The following specification has been developed by

Marlite

202 Harger St.

Dover, Ohio 44622

Tel: (330) 343-6621 Fax: (330) 343-4668.

Email:  info@marlite.com  www.marlite.com

to assist Architects and Designers in the specification of Decorative Fiberglass Reinforced Plastic wall panel system for high wear areas.  FRP Panels are excellent for sanitary environments because they facilitate washing and cleaning and do not support mold or mildew growth.  However, FRP panels are subject to the effects of continuous humidity and temperature.  Provide adequate ventilation for drying and do not use in panels in high temperature areas.

Marlite Artizan FRP panels offer a superb array of decorative printed rotogravure finishes with exceptional image integrity; unlimited varieties of woodgrain and abstract pattern plus tactile as well as visual textures.  Custom designs and matching designs are available upon request

Marlite Envue Graphic FRP provides impressive visuals of high-resolution photographs, illustrations, logos, tile designs and custom graphics, all protected by Marlite’s tough Sani-Coat sealer. A special application process produces optimum graphic reproduction on a tough, sanitary surface.

Marlite Symmetrix with Sani-Coat FRP panels feature prefinished precision grid score lines that provide the look of tile without grout to clean or deteriorate.  Custom designs and matching designs are available upon request.

.

The section has been formatted in accordance with the principals embodied in the Construction Specifications  Institute's  Manual of Practice and is intended for use in conjunction with Contract Conditions, Bidding Conditions and General Requirements developed in accordance with CSI guidelines.

Notes to the specifier are included in the boxes. Options that must be selected by the specifier are shown in brackets [         ].   Inapplicable clauses shall be deleted.

SECTION 09 7720 – DECORATIVE FIBERGLASS REINFORCED WALL PANELS

GENERAL

SUMMARY

Section Includes:   Prefinished polyester glass reinforced plastic sheets and adhered to unfinished [gypsum] [cementitous] [untreated plywood] wallboard.

[Aluminum] [PVC] trim.

[PVC Wall base.]

Products Not Furnished or Installed under This Section:

Gypsum [Cementitious] substrate board.

Resilient Base.

RELATED SECTIONS

Section [____] – 	Gypsum [Cementitious] substrate board.

Section [____] - Wood [Metal] Stud Framing

Section [____] - Painting & Transparent Finishes.

Section [____] - Resilient Base.

REFERENCES

References are listed as a convenience and are often deleted in their entirety.  If required by the user agency delete references from the list below that are not actually required by the text of the edited section

American Society for Testing and Materials:  Standard Specifications (ASTM)

ASTM D 256 -	Izod Impact Strengths (ft #/in)

ASTM D 570 -	Water Absorption (%)

ASTM D 638 -	Tensile Strengths (psi) & Tensile Modulus (psi)

ASTM D 790 -	Flexural Strengths (psi) & Flexural Modulus (psi)

ASTM D 2583- Barcol Hardness

ASTM D 5319 - Standard Specification for Glass-Fiber Reinforced Polyester Wall and Ceiling Panels.

ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

SUBMITTALS

Product Data:  Submit sufficient manufacturer's data to indicate compliance with these specifications, including:

Preparation instructions and recommendations.

Storage and handling requirements and recommendations.

Installation methods.

Shop Drawings:  Submit elevations of each wall showing location of paneling and trim members with respect to all discontinuities in the wall elevation.

Selection Samples:  Submit manufacturer’s standard color pattern selection samples representing manufacturer's full range of available colors and patterns.

Samples for Verification:   Submit appropriate section of panel for each finish selected indicating the color, texture, and pattern required.

Submit complete with specified applied finish.

For selected patterns show complete pattern repeat.

Exposed Molding and Trim:  Provide samples of each type, finish, and color.

Manufacturers Material Safety Data Sheets (MSDS) for adhesives and sealants prior to their delivery to the site.

QUALITY ASSURANCE

Conform to building code requirements for interior finish for smoke and flame spread requirements as tested in accordance with:

ASTM E 84 (Method of test for surface burning characteristics of building Materials)

Wall Required Rating – Class [A] [C].

Include the following if products are used in areas subject to stringent wash down requirements.

### Sanitary Standards:  System components and finishes to comply with:

United States Department of Agriculture (USDA) requirements for food preparation facilities, incidental contact.

#### Food and Drug Administration (FDA) 1999 Food Code 6-101.11.

Canadian Food Inspection Agency (CFIA) requirements.

DELIVERY, STORAGE AND HANDLING

Deliver materials factory packaged on strong pallets.

Store panels and trim lying flat, under cover and protected from the elements.  Allow panels to acclimate to room temperature (70°) for 48 hours prior to installation.

PROJECT CONDITIONS

Environmental Limitations:  Building are to be fully enclosed prior to installation with sufficient heat (70°) and ventilation consistent with good working conditions for finish work

During installation and for not less than 48 hours before, maintain an ambient temperature and relative humidity within limits required by type of adhesive used and recommendation of adhesive manufacturer.

Provide ventilation to disperse fumes during application of adhesive as recommended by the adhesive manufacturer.

WARRANTY

Furnish one year guarantee against defects in material and workmanship.

PRODUCTS

ACCEPTABLE MANUFACTURER

Marlite;   202 Harger Street, Dover, OH  44622.  800-377-1221  FAX (330) 343-4668 Email:  info@marlite.com www.marlite.com.

Product:

Artizan FRP with Sani-Coat.

Envue with Sani-Coat.

Symmetrix with Sani-Coat.

PANELS

Fiberglass reinforced thermosetting polyester resin panel sheets complying with ASTM D 5319.

Coating:  Multi layer print, primer and finish coats.

Dimensions:

Thickness – 0.090 inch (2.29mm) nominal

Width - 4'-0”  (1.22m) nominal

Length – [10’-0” (3.0m)][8’-0” (2.4m) ][As indicated on the drawings] nominal

Tolerance:

Length and Width:  +/-1/8 inch (3.175mm)

Square -  Not to exceed 1/8 inch for 8 foot (2.4m) panels or 5/32 inch (3.96mm) for 10 foot (2.4m) panels

Properties:  Resistant to rot, corrosion, staining, denting, peeling, and splintering.

Flexural Strength - 1.0 x 104 psi per ASTM D 790. (7.0 kilogram-force/square millimeter)

Flexural Modulus - 3.1 x 105 psi per ASTM D 790. (217.9 kilogram-force/square millimeter)

Tensile Strength - 7.0 x 103 psi per ASTM D 638. (4.9 kilogram-force/square millimeter)

Tensile Modulus - 1.6 x 105 psi per ASTM D 638. (112.5 kilogram-force/square millimeter)

Water Absorption - 0.72% per ASTM D 570.

Barcol Hardness (scratch resistance) of 35 55 as per ASTM D 2583.

Izod Impact Strength of 72 ft. lbs./in ASTM D 256

Back Surface:  Smooth.  Imperfections which do not affect functional properties are not cause for rejection.

Select finish from our full Marlite Finish Palette at www.marlite.com or contact Marlite to create your own Finish.

Front Finish: [As Indicated on the Drawings] [In accordance with preapproved sample.  Information available from the Architect’s Office][ __________________________________}

Specifier Note: Marlite’s FRP & Symmetrix with Sani-Coat Panels are available in 						several configurations, including Class A (I) and Class C (III) Fire-rated, along 						with various surface textures for both FRP & Symmetrix with Sani-Coat.  Symmetrix 					with Sani-Coat are available with standard surface grooving and customized groove 						layouts to match architectural specifications.

        - Color: [Specifier to choose.] Marlite FRP is available in a variety of colors, including 100 White, 106 Beige, 118 Natural Almond, 140 Ivory, 145 Silver, 151 Light Grey, P807 Black & 199 Bright White. Special colors can be custom matched and manufactured provided there is a minimum square footage order of 5,000 ft2.  Contact Marlite for lead time.

        - Surface [Specifier to choose.] Marlite FRP is available on two standard surface textures. Pebbled (indicated by “P” designation i.e., P 100 White) and Smooth (indicated by “S” designation i.e., S 100 White).

        - Fire Rating [Specifier to choose.] Marlite FRP is available in either Class A (I) or Class C (III) Fire Rating.  Specifier should add designation to product number only for Class A (i.e., P 100 White, Class A).

        - Size: [Specifier to choose, or as indicated on drawings.] Marlite FRP standard sizes are;

          - 4’ x 8’ [1.2m x 2.4m] x .120”

          - 4’ x 9’ [1.2m x 2.7m] x .120”

          - 4’ x 10’ [1.2m x 3m] x .120”

          - Ceiling panels (designed for suspended ceiling installation)

- 23 ¾” x 47 ¾” (0.6m x 1.2m) x .120”

- 23 ¾” x 23 ¾” (0.6m x 0.6m) x .120”

Can be specified as FRP panels only or backed with 5/8” FR Drywall.

Delete the following if resilient bases are used

BASE

Marlite Base Molding for 0.090 inch (2.29mm) thick FRP Panels

Color: [Black] [Quarry Red].

Profiles:

M 612 FRP Base Molding

M 651 Inside Corner

M 660 Outside Corner

M 620 LH End Cap

M 625 RH End Cap

MOLDINGS

Select PVC or Aluminum trim for Envue and Symmetrix systems.  PVC trims are not available on Artisan.

Aluminum Trim:  Heavy weight extruded aluminum 6063-T5 alloy prefinished at the factory.

Finish:  Factory oven-baked finish.

Profiles	:

The following are Symmetrix and Envue trim profiles.

F 550 Inside Corner

F 561 Outside Corner

F 565 Division

F 570 Edge

The following are Artisan trim profiles.

A551 Inside Corner.

A560 Outside Corner

A565 Division

A570 Edge

Color:  [Bright Anodized] _____________

PVC colors are available to coordinate with Sani-Coat colorways.  See current Marlite Finish Guide for available choice.

        - PVC:  Extruded PVC Trim Profiles for .090 inch thick panels.

M 350 Inside Corner

M 360 Outside Corner

M 365 Division

M 370 Edge

Color:  ________________

Outside Corner Guard:

F 560 Stainless Steel

Finish:  #4 satin

M 961 PVC

199 White

118 Natural Almond

140 Ivory

145 Silver

151 Light Grey

ACCESSORIES

Specify rivets for use in areas with dramatic changes in temperature and/or humidity, where the substrate is unusually uneven, and in all low temperatures or cold storage applications.

Fasteners:  Non-staining nylon drive rivets.

Match panel colors.

Length to suit project conditions.

Adhesive:  Either of the following construction adhesives complying with ASTM C 557.

Marlite C-551 FRP Adhesive  - Water- resistant, non-flammable adhesive

Marlite C-375 Construction adhesive flexible, water-resistant, solvent based adhesive formulated for fast, easy application.

Sealant:

Marlite Brand MS-250 Clear Silicone Sealant

Marlite Brand MS-251 White Silicone Sealant

Colors available to coordinate with Marlite Artizan colorways..

Marlite Brand - Color Match Sealant,

EXECUTION

PREPARATION

Examine backup surfaces to determine that corners are plumb and straight, surfaces are smooth, uniform, clean and free from foreign matter, nails countersunk, joints and cracks filled flush and smooth with the adjoining surface.

Verify that stud spacing does not exceed 24 inch (61cm) on-center.

Repair defects prior to installation.

Level wall surfaces to panel manufacturer’s requirements.  Remove protrusions and fill indentations.

INSTALLATION

Comply with manufacturer's recommended procedures and installation sequence.

Cut sheets to meet supports allowing 1/8” inch (3 mm) clearance for every 8 foot (2.43m) of panel.

Cut and drill with carbide tipped saw blades or drill bits, or cut with shears.

Pre-drill fastener holes 1/8 inch (3.175mm) oversize with high speed drill bit.

Space at 8 inches (20.32cm) maximum on center at perimeter, approximately 1 inch from panel edge.

Space at in field in rows 16 inches (40.64cm) on center, with fasteners spaced at 12 inches (30.48 cm) maximum on center.

Apply panels to board substrate, above base, vertically oriented with seams plumb and pattern aligned with adjoining panels.

Install panels with manufacturer's recommended gap for panel field and corner joints.

Adhesive trowel and application method to conform to adhesive manufacturer’s recommendations.

Drive fasteners for snug fit.  Do not over-tighten.

Apply panel moldings to all panel edges using silicone sealant providing for required clearances.

All moldings must provide for a minimum 1/8 inch (3.18mm) of panel expansion at joints and edges, to insure proper installation.

Apply sealant to all moldings, channels and joints between the system and different materials to assure watertight installation.

CLEANING

Remove excess sealant from panels and moldings.  Wipe panel down using a damp cloth and mild soap solution or cleaner.

Refer to manufacturer's specific cleaning recommendations Do not use abrasive cleaners.

END OF SECTION 09 7720