Note:

This document contains information and notes in hidden text.

If you need assistance to view & hide text, instructions are at this link:

http://www.marlite.com/hidden-notes-instructions.aspx

Delete this note and hyperlink after editing is complete.

The following specification has been developed by

Marlite

202 Harger St.

Dover, Ohio 44622

Tel: (330) 343-6621 Fax: (330) 343-4668.

Email:  info@marlite.com  www.marlite.com

to assist Architects and Designers in the specification of Decorative Fiberglass Reinforced Plastic wall panel system for high wear areas.

Marlite Stamdard FRP Panels are excellent for sanitary environments since they facilitate washing and cleaning and do not support mold or mildew growth.  However, FRP panels are subject to the effects of continuous humidity and temperature.  Provide adequate ventilation for drying and do not use in high temperature areas.

Marlite Induro FRP provides an exceptionally wear resistant decorative panel; due to an exclusive process of thermally bonding melamine impregnated surfacing materials directly to the FRP core.  Designed to match or coordinate with popular High Pressure Laminates, these panels offer a superb array of decorative finishes and patterns from solid colors to wood-grains and abstract patterns.  Custom color and patterns are available upon request.

Marlite Artizan FRP panels offer a superb array of decorative printed rotogravure finishes with exceptional image integrity; unlimited varieties of woodgrain and abstract pattern plus tactile as well as visual textures.  Custom color and patterns are available upon request.

Marlite Envue Graphic FRP provides impressive visuals of high-resolution photographs, illustrations, logos, tile designs and custom graphics, all protected by Marlite’s tough Sani-Coat sealer. A special application process produces optimum graphic reproduction on a tough, sanitary surface.

Marlite Symmetrix with Sani-Coat FRP panels feature prefinished precision grid score lines that provide the look of tile without grout to clean or deteriorate.  Custom color and patterns are available upon request.

The section has been formatted in accordance with the principals embodied in the Construction Specifications  Institute's  Manual of Practice and is intended for use in conjunction with Contract Conditions, Bidding Conditions and General Requirements developed in accordance with CSI guidelines.

Notes to the specifier are included. Options that must be selected by the specifier are shown in brackets [         ].   Inapplicable clauses shall be deleted.

SECTION 09 7720 – DECORATIVE FIBERGLASS REINFORCED WALL PANELS

GENERAL

SUMMARY

Section Includes:   Prefinished polyester glass reinforced plastic sheets and adhered to unfinished [gypsum] [cementitous] [untreated plywood] wallboard.

[Aluminum] [PVC] trim.

[PVC Wall base.]

Products Not Furnished or Installed under This Section:

Gypsum [Cementitious] substrate board.

Resilient Base.

RELATED SECTIONS

Section [____] – 	Gypsum [Cementitious] substrate board.

Section [____] - Wood [Metal] Stud Framing

Section [____] - Painting & Transparent Finishes.

Section [____] - Resilient Base.

REFERENCES

References are listed as a convenience and are often deleted in their entirety.  If required by the user agency delete references from the list below that are not actually required by the text of the edited section.

American Society for Testing and Materials:  Standard Specifications (ASTM)

ASTM D 256 -	Izod Impact Strengths (ft #/in)

ASTM D 570 -	Water Absorption (%)

ASTM D 638 -	Tensile Strengths (psi) & Tensile Modulus (psi)

ASTM D 790 -	Flexural Strengths (psi) & Flexural Modulus (psi)

ASTM D 2583- Barcol Hardness

ASTM D 5319 - Standard Specification for Glass-Fiber Reinforced Polyester Wall and Ceiling Panels.

ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

SUBMITTALS

Product Data:  Submit sufficient manufacturer's data to indicate compliance with these specifications, including:

Preparation instructions and recommendations.

Storage and handling requirements and recommendations.

Installation methods.

Shop Drawings:  Submit elevations of each wall showing location of paneling and trim members with respect to all discontinuities in the wall elevation.

Selection Samples:  Submit manufacturer’s standard color pattern selection samples representing manufacturer's full range of available colors and patterns.

Samples for Verification:   Submit appropriate section of panel for each finish selected indicating the color, texture, and pattern required.

Submit complete with specified applied finish.

For selected patterns show complete pattern repeat.

Exposed Molding and Trim:  Provide samples of each type, finish, and color.

Manufacturers Material Safety Data Sheets (MSDS) for adhesives, sealants and other pertinent materials prior to their delivery to the site (available as downloads for most Marlite’s products at http://www.marlite.com/tech-details.aspx or by contacting Marlite at info@marlite.com).

QUALITY ASSURANCE

Conform to building code requirements for interior finish for smoke and flame spread requirements as tested in accordance with:

ASTM E 84 (Method of test for surface burning characteristics of building Materials)

Wall Required Rating – Class [A] [C].

Include the following if products are used in areas subject to stringent wash down requirements.

### Sanitary Standards:  System components and finishes to comply with:

United States Department of Agriculture (USDA) requirements for food preparation facilities, incidental contact.

#### Food and Drug Administration (FDA) 1999 Food Code 6-101.11.

Canadian Food Inspection Agency (CFIA) requirements.

DELIVERY, STORAGE AND HANDLING

Deliver materials factory packaged on strong pallets.

Store panels and trim lying flat, under cover and protected from the elements.  Allow panels to acclimate to room temperature (70°) for 48 hours prior to installation.

PROJECT CONDITIONS

Environmental Limitations:  Building are to be fully enclosed prior to installation with sufficient heat (70°) and ventilation consistent with good working conditions for finish work

During installation and for not less than 48 hours before, maintain an ambient temperature and relative humidity within limits required by type of adhesive used and recommendation of adhesive manufacturer.

Provide ventilation to disperse fumes during application of adhesive as recommended by the adhesive manufacturer.

WARRANTY

Furnish one year guarantee against defects in material and workmanship.

PRODUCTS

ACCEPTABLE MANUFACTURER

Marlite;   202 Harger Street, Dover, OH  44622.  800-377-1221 FAX (330) 343-4668 Email:  info@marlite.com www.marlite.com.

Product:

Standard FRP

Induro FRP

Artizan FRP with Sani-Coat.

Envue with Sani-Coat.

Symmetrix with Sani-Coat.

PANELS

Fiberglass reinforced thermosetting polyester resin panel sheets complying with ASTM D 5319.

Coating:  Multi-layer print, primer and finish coats or applied over-layer.

Dimensions:

Thickness – 0.090 “ (2.29mm) nominal

Width - 4'-0”  (1.22m) nominal

Induro FRP Panels are not available in lengths exceeding 8’ (2.4m).

Length – [10’-0” (3.0m)][8’-0” (2.4m) ][As indicated on the drawings] nominal

Tolerance:

Length and Width:  +/-1/8 “ (3.175mm)

Square -  Not to exceed 1/8 “ for 8 foot (2.4m) panels or 5/32 “ (3.96mm) for 10 foot (2.4m) panels

Properties:  Resistant to rot, corrosion, staining, denting, peeling, and splintering.

Flexural Strength - 1.0 x 104 psi per ASTM D 790. (7.0 kilogram-force/square millimeter)

Flexural Modulus - 3.1 x 105 psi per ASTM D 790. (217.9 kilogram-force/square millimeter)

Tensile Strength - 7.0 x 103 psi per ASTM D 638. (4.9 kilogram-force/square millimeter)

Tensile Modulus - 1.6 x 105 psi per ASTM D 638. (112.5 kilogram-force/square millimeter)

Water Absorption - 0.72% per ASTM D 570.

Barcol Hardness (scratch resistance) of 35 55 as per ASTM D 2583.

Izod Impact Strength of 72 ft. lbs./in ASTM D 256

Back Surface:  Smooth.  Imperfections which do not affect functional properties are not cause for rejection.

Select finish from our full Marlite Finish Palette at www.marlite.com or contact Marlite to create your own finish.

Front Finish: [As Indicated on the Drawings] [In accordance with preapproved sample.  Information available from the Architect’s Office][ __________________________________}

Specifier Note: Marlite’s Standard FRP, Induro FRP, Artizan FRP, Envue FRP & Symmetrix with Sani-Coat Panels are available in several configurations, including Class A (I) and Class C (III) Fire-rated, along with various surface textures for both Standard FRP & Symmetrix with Sani-Coat.  All Marlite FRP products can be made available with standard surface grooving and customized groove layouts to match architectural specifications.

        - Color: [Specifier to choose.]

Marlite Standard FRP is available in a variety of colors, including;

100 White

106 Beige,

118 Natural Almond

140 Ivory

145 Silver

151 Light Grey

P807 Black

199 Bright White

Custom patterns and colors are available.  Minimum quantities may apply.  Contact a Marlite representative for details.

Marlite Induro FRP is available in a variety of colors and patterns, including;

D354 Designer White

D381 Fashion Grey

FP610 Hard Rock Maple

FP612 Graphite Spectrum

4143 Neutral Glace

4745 Maroochy Brush

4746 Woolamai Brush

4810 Titanium

4873 Western Bronze

4878 Pewter Mesh

4893 Tumbled Mosiac

7061 Natural Pear

7922 Brighton Walnut

7924 Biltmore Cherry

7925 Monticello Maple

7939 Blonde Echo

Custom patterns and colors are available.  Minimum quantities may apply.  Contact a Marlite representative for details.

Marlite Artizan FRP is available in a variety of colors and patterns, including;

148 Monticello Anigre

310 Sierra Maple

715 Mahogany

925 Autumn Cherry

5408 Monterey Sand

5409 Townsend

5410 Sebring

5411 Rainier

194 Cody

192 Laramie

209 Adara

211 Grizel

181-G1212 Dusk

182-G1212 Oxide

5415-G88 Coronado

5416-G88 Catalina

T936-G44 Milan

T938-G44 Tuscany

T938-G88 Tuscany

T939-G44 Verona

T939-G88 Verona

T5412-G1212 Palermo

T5413-G1212 Genoa

T5414-G88 Modena

T5417-G88 Salerno

T5418-G88 Tangier

T5419-G88 Madras

T5420-G88 Ceylon

Custom patterns and colors are available.  Minimum quantities may apply.  Contact a Marlite representative for details.

Marlite Envue FRP includes full custom graphics capabilities and are provided as;

Customer supplied artwork, in a digital file format compatible with Marlite’s requirements and in a layout compatible with the panel dimensions as required for the installation.  Revisions by Marlite Graphics Services to customer supplied artwork are to be submitted for customer approval.  It is the customer’s responsibility to contact their Marlite representative for Marlite’s digital file format requirements. Charges may apply if revisions are required to re-format artwork files.

Marlite supplied artwork, for customer review and approval.  Graphic serviced and set-up charges may apply.

Marlite Symmetrix with Sani-Coat FRP is available in a variety of colors, patterns and groove configurations, including;

C100-G44 White

C100-G66 White

C118-G44 Almond

C140-G44 Ivory

C145-G44 Silver

C105-G44 Black

C131-G44 Everglade

C133-G44 Periwinkle

C150-G44 White with Black

C151-G44 White with Everglade

C153-G44 White with Periwinkle

Custom patterns and colors are available.  Minimum quantities may apply.  Contact a Marlite representative for details.

        - Surface [Specifier to choose.] Marlite Standard FRP and Symmetrics are available on two standard surface textures. Pebbled (indicated by “P” designation i.e., P 100 White) and Smooth (indicated by “S” designation i.e., S 100 White).  All other Marlite FRP products are smooth surface texture.

        - Fire Rating [Specifier to choose.] Marlite FRP is available in either Class A (I) or Class C (III) Fire Rating.  Specifier should add designation to product number only for Class A (i.e., P 100 White, Class A).

        - Size: [Specifier to choose, or as indicated on drawings.] standard sizes are;

          - Marlite FRP / Symmetrics / Artizan / Envue

            - 48” x 96” [1.2m x 2.4m] x .090” (3mm) nom.

            - 48” x 108” [1.2m x 2.7m] x .090” (3mm) nom.

            - 48” x 120” [1.2m x 3m] x .090” (3mm) nom.

          - Marlite Induro FRP

            - 47.5” x 95.5” [1.2m x 2.4m] x .090” (3mm) nom.

          - Ceiling panels (designed for suspended ceiling installation)

- 23 ¾” x 47 ¾” (0.6m x 1.2m) x  .090” (3mm)

- 23 ¾” x 23 ¾” (0.6m x 0.6m) x  .090” (3mm)

Can be specified as FRP panels only or backed with 5/8” FR Drywall.

Delete the following if resilient or contractor supplied bases are used.

BASE

Marlite Base Molding for 0.090 “ (2.29mm) thick FRP Panels

Color: [Black] [Quarry Red].

Profiles:

M 612 FRP Base Molding, 10’ length

M 651 Inside Corner

M 660 Outside Corner

M 620 LH End Cap

M 625 RH End Cap

MOLDINGS

Select PVC or Aluminum trims.

Aluminum Trim:  Heavy weight extruded aluminum 6063-T5 alloy prefinished at the factory.

Profiles	:

The following are extruded aluminum trim profiles.

F 550 Inside Corner, 8’ length

F 561 Outside Corner, 8’ length

F 565 Division, 8’ length

F 570 Edge, 8’ length

Color: Brite Anodized

The following are extruded aluminum trim profiles.

Aluminum Trim:  Heavy weight extruded aluminum 6063-T5 alloy prefinished at the factory.

A551Inside Corner, 8’ length

A560 Outside Corner, 8’ length

A565 Division, 8’ length

A570 Edge, 8’ length

Color:  [Factory Oven-Baked Finish to match spec’d panel][Black Satin Anodized][Clear Satin Anodized]

The following are extruded PVC trim profiles. PVC colors are also available to coordinate with Sani-Coat colorways.  See current Marlite Finish Guide for available choice.

PVC Trim:  Thin-wall semi-rigid extruded PVC.

M 350 Inside Corner, [8’ length][10’ length]

M 360 Outside Corner, [8’ length][10’ length]

M 365 Division, [8’ length][10’ length]

M 370 Edge, [8’ length][10’ length]

Color:  [White][Beige][Natural Almond][Ivory][Silver][Light Grey][Black]

The following are dual-durometer extruded polypropylene trim profiles with Marlite’s exclusive Dual-Seal Technology, designed to restrict the growth and propagation of harmful pathogens. Standard colorways are extruded with color throughout the profile.

SaniSeal Trim: Co-extruded, dual-durometer polypropylene/monprene profiles with Dual-Seal Technology and high-performance pressure sensitive adhesive.

S650 Inside Corner, 10’ length

S660 Outside Corner, 10’ length

S665 Division, 8’ length

S670 Edge, 10’ length

Color: [White][Umber][Slate][Tan][Black][Custom, per specification]

Outside Corner Guard:

F 560SS Stainless Corner Guard, [8’ length][10’ length]

Finish:  #4 brushed satin

M 961 PVC Outside Corner Guard

Color: [White, [8’ length][10’ length]][Natural Almond, [8’ length][10’ length]][Ivory, 10’ length][Silver, 10’ length][Light Grey, 10’ length]

ACCESSORIES

Specify rivets for use in areas with dramatic changes in temperature and/or humidity, where the substrate is unusually uneven, and in all low temperatures or cold storage applications.

Fasteners:  Non-staining nylon drive rivets.

Match panel colors.

Length to suit project conditions.

Adhesive:  Either of the following construction adhesives complying with ASTM C 557.

Marlite C-551 FRP Adhesive - Water- resistant, non-flammable adhesive.

Marlite C-375 Construction Adhesive - Flexible, water-resistant, solvent based adhesive, formulated for fast, easy application.

Titebond Advanced Polymer Panel Adhesive – VOC compliant, non-flammable, environmentally safe adhesive.

Sealant:

Marlite Brand MS-250 Clear Silicone Sealant.

Marlite Brand MS-251 White Silicone Sealant.

Colors are available to coordinate with Marlite Artizan colorways.

Marlite Brand - Color Match Sealant .

EXECUTION

PREPARATION

Examine backup surfaces to determine that corners are plumb and straight, surfaces are smooth, uniform, clean and free from foreign matter, nails countersunk, joints and cracks filled flush and smooth with the adjoining surface.

Verify that stud spacing does not exceed 24” (61cm) on-center.

Repair defects prior to installation.

Level wall surfaces to panel manufacturer’s requirements.  Remove protrusions and fill indentations.

INSTALLATION

Comply with manufacturer's recommended procedures and installation sequence.

Cut sheets to meet supports allowing 1/8” (3 mm) clearance for every 8 foot (2.4m) of panel.

Cut and drill with carbide tipped saw blades or drill bits, or cut with shears.

Pre-drill fastener holes 1/8” (3mm) oversize with high speed drill bit.

Space at 8” (200mm) maximum on center at perimeter, approximately 1” from panel edge.

Space at in field in rows 16’ (40.64cm) on center, with fasteners spaced at 12” (30.48 cm) maximum on center.

Apply panels to board substrate, above base, vertically oriented with seams plumb and pattern aligned with adjoining panels.

Install panels with manufacturer's recommended gap for panel field and corner joints.

Adhesive trowel and application method to conform to adhesive manufacturer’s recommendations.

Drive fasteners for snug fit.  Do not over-tighten.

Apply panel moldings to all panel edges using silicone sealant providing for required clearances.

All moldings must provide for a minimum 1/8 “ (3mm) of panel expansion at joints and edges, to insure proper installation.

Apply sealant to all moldings, channels and joints between the system and different materials to assure watertight installation.

CLEANING

Remove excess sealant from panels and moldings.  Wipe panel down using a damp cloth and mild soap solution or cleaner.

Refer to manufacturer's specific cleaning recommendations Do not use abrasive cleaners.

END OF SECTION 09 7720