Note:

This document contains information and notes in hidden text.

If you need assistance to view & hide text, instructions are at this link:

http://www.marlite.com/hidden-notes-instructions.aspx

Delete this note and hyperlink after editing is complete.

The following specification has been developed by

Marlite

202 Harger St.

Dover, Ohio 44622

Tel: (330) 343-6621 Fax: (330) 343-4668.

Email:  info@marlite.com  www.marlite.com

to assist Architects and Designers in the specification of Decorative Fiberglass Reinforced Plastic wall panel system for high wear areas.

Marlite Stamdard FRP Panels are excellent for sanitary environments since they facilitate washing and cleaning and do not support mold or mildew growth.  However, FRP panels are subject to the effects of continuous humidity and temperature.  Provide adequate ventilation for drying and do not use in high temperature areas.

Marlite Induro FRP provides an exceptionally wear resistant decorative panel; due to an exclusive process of thermally bonding melamine impregnated surfacing materials directly to the FRP core.  Designed to match or coordinate with popular High Pressure Laminates, these panels offer a superb array of decorative finishes and patterns from solid colors to wood-grains and abstract patterns.  Custom color and patterns are available upon request.

Marlite Artizan FRP panels offer a superb array of decorative printed rotogravure finishes with exceptional image integrity; unlimited varieties of woodgrain and abstract pattern plus tactile as well as visual textures.  Custom color and patterns are available upon request.

Marlite Envue Graphic FRP provides impressive visuals of high-resolution photographs, illustrations, logos, tile designs and custom graphics, all protected by Marlite’s tough Sani-Coat sealer. A special application process produces optimum graphic reproduction on a tough, sanitary surface.

Marlite Symmetrix with Sani-Coat FRP panels feature prefinished precision grid score lines that provide the look of tile without grout to clean or deteriorate.  Custom color and patterns are available upon request.

The section has been formatted in accordance with the principals embodied in the Construction Specifications  Institute's  Manual of Practice and is intended for use in conjunction with Contract Conditions, Bidding Conditions and General Requirements developed in accordance with CSI guidelines.

Notes to the specifier are included. Options that must be selected by the specifier are shown in brackets [         ].   Inapplicable clauses shall be deleted.

SECTION 09 7720 – DECORATIVE FIBERGLASS REINFORCED WALL PANELS

GENERAL

SUMMARY

Section Includes:   Prefinished polyester glass reinforced plastic sheets and adhered to unfinished [gypsum] [cementitous] [untreated plywood] wallboard.

[PVC] trim.

[PVC] Wall base.

Products Not Furnished or Installed under This Section:

Gypsum [Cementitious] substrate board.

Resilient Base.

RELATED SECTIONS

Section [____] – Gypsum [Cementitious] substrate board.

Section [____] - Wood [Metal] Stud Framing

Section [____] - Painting & Transparent Finishes.

Section [____] - Resilient Base.

REFERENCES

References are listed as a convenience and are often deleted in their entirety.  If required by the user agency delete references from the list below that are not actually required by the text of the edited section.

American Society for Testing and Materials:  Standard Specifications (ASTM)

ASTM D 790 – Flexural Strengths (psi)

ASTM D 790 – Flexural Modulus (psi)

ASTM D 638 – Tensile Strengths (psi)

ASTM D 638 – Tensile Modulus (psi)

ASTM D 2583 – Barcol Hardness

ASTM D 256 -	Izod Impact Strengths (ft #/in)

ASTM D 696 – Thermal Coefficient of Lineal Expansion (in/in/F)

ASTM D 570 – Water Absorption (%)

ASTM D 792 – Specific Gravity

ASTM D 3359 – Cross-cut Adhesion

ASTM D 3273 – Mold & Mildew

ASTM D 5319 - Standard Specification for Glass-Fiber Reinforced Polyester Wall and Ceiling Panels.

ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

SUBMITTALS

Product Data:  Submit manufacturer's data to indicate compliance with these specifications, including:

Storage, handling and preparation instructions and recommendations.

Installation instructions.

Shop Drawings:  Submit elevations of each wall showing location of paneling and trim members with respect to all discontinuities in the wall elevation.

Selection Samples:  Submit manufacturer’s standard color pattern selection samples representing manufacturer's full range of available colors and patterns.

Samples for Verification:   Submit appropriate section of panel for each finish selected indicating the color, texture, and pattern required.

Submit complete with specified applied finish.

For selected patterns show complete pattern repeat.

Exposed Trim Molding:  Provide samples of each type, finish, and color.

Manufacturers Safety Data Sheets (SDS) for adhesives, sealants and other pertinent materials prior to their delivery to the site (available as downloads for most Marlite’s products at http://www.marlite.com/tech-details.aspx or by contacting Marlite at info@marlite.com).

QUALITY ASSURANCE

Conform to building code requirements for interior finish for smoke and flame spread requirements as tested in accordance with:

ASTM E 84 (Method of test for surface burning characteristics of building Materials)

Wall Required Rating – Class [C].

Include the following if products are used in areas subject to stringent wash down requirements.

### Sanitary Standards:  System components and finishes to comply with:

United States Department of Agriculture (USDA) / Food Safety & Inspection Services (FSIS) requirements for food preparation facilities, incidental contact.

#### Food and Drug Administration (FDA) 2013 Food Code 6-101.11.

Canadian Food Inspection Agency (CFIA) requirements.

DELIVERY, STORAGE AND HANDLING

Deliver materials factory packaged on strong pallets.

Store panels and trim lying flat, under cover and protected from the elements.  Allow panels and adhesive to acclimate to room temperature (range of 60 to 75°F) for 48 hours prior to installation.

PROJECT CONDITIONS

Environmental Limitations:  Building are to be fully enclosed prior to installation with heat (70° or similar room temperature) and ventilation consistent with good working conditions for finish work.

During installation and for not less than 48 hours before, maintain an ambient temperature and relative humidity within limits required by type of adhesive used and recommendation of adhesive manufacturer.

Provide ventilation to disperse fumes during application of adhesive as recommended by the adhesive manufacturer.

WARRANTY

Furnish one-year guarantee against defects in material.

PRODUCTS

ACCEPTABLE MANUFACTURER

Marlite; 1 Marlite Drive, Dover, OH  44622.  800-377-1221 FAX (330) 343-4668 Email:  info@marlite.com www.marlite.com.

Product:

Symmetrix™ FRP Panels with Sani-coat Sealer

Symmetrix™ SmartSeam FRP Panels with Sani-coat Sealer

PANELS

Fiberglass reinforced thermosetting polyester resin panel sheets complying with ASTM D 5319.

Finishing:  BlueSky™ Advanced Finishing System:  Spray-applied Sani-coat Sealer covers entire panel including grooves and features water-based coatings and controlled, low-temperature inline curing.

Dimensions:

Thickness – 0.090” (2.29mm) nominal

Width - 4'-0” (1.22m) nominal

Induro FRP Panels are not available in lengths exceeding 8’ (2.4m).

Length – [4’-0” (1.22m)] [8’-0” (2.4m)][10’-0” (3.0m)] [As indicated on the drawings] nominal

Tolerance:

Length and Width:  +/-1/8” (3.175mm)

Square - Not to exceed 1/8” for 4’ (1.2m) panels, 8’ (2.4m) panels or 5/32” (3.96mm) for 10’ (3.0m) panels

Properties:  Resistant to rot, corrosion, denting, peeling, and splintering.

1.	Flexural Strength – 0.9 x 104 psi per ASTM D 790.

2.	Flexural Modulus – 6.0 x 106 psi per ASTM D 790.

3.	Tensile Strength – 11.5 x 103 psi per ASTM D 638.

4.	Tensile Modulus – 0.45 x 106 psi per ASTM D 638.

5.	Barcol Hardness (scratch resistance) – 28 per ASTM D 2583.

6.	Izod Impact Strength – 6.0 ft. lbs./in ASTM D 256

7.	Thermal Coefficient of Lineal Expansion – 2.22 x 10-5 in/in/F per ASTM D 696

8.	Water Absorption – 0.15% per ASTM D 570.

9. 	Specific Gravity – 1.8 per ASTM D 792.

10.	Cross-cut Adhesion – 0 removed per ASTM D 3359

11.	Mold & Mildew – Pass per ASTM D 3273.

          - Standard Specification for FRP Wall Panels – per ASTM D 5319

Standard Test Method Surface Burning Characteristics of Building Materials – Class C per ASTM E 84.

Back Surface:  Smooth.  Imperfections which do not affect functional properties are not cause for rejection.

Select finish from our full Marlite Finish Palette at www.marlite.com or contact Marlite to create your own finish.

Front Finish: [As Indicated on the Drawings] [In accordance with pre-approved sample.  Information available from the Architect’s Office] [ __________________________________}

Specifier Note: Marlite’s Symmetrix FRP Panels and Symmetrix SmartSeam FRP Panels with BlueSky Advanced Finishing are available in Class C (III) Fire-ratings.  Symmetrix FRP Panels and Symmetrix SmartSeam FRP Panels can be made available with standard surface groove and customized groove layouts to match architectural specifications.

        - Color: [Specifier to choose.]

Marlite Symmetrix SmartSeam FRP Panels with Sani-coat Sealer are available in a variety of colors, pattern designs, graphics and images and scoring configurations, including:

SYM SS100-G63 White (6” x 3” subway groove configuration)

SYM SS916-G63 White w/ Black grooves (6” x 3” subway groove configuration)

SYM SS105-G63 Black w/ White grooves (6” x 3” subway groove configuration)

SYM SS100-G44 White (4” x 4” square groove configuration)

SYM SS916-G44 White w/ Black grooves (4” x 4” groove configuration)

SYM SS105-G44 Black w/ White grooves (4” x 4” square groove configuration)

SYM SS100-G3H6 White (3” x 6 sides hexagon groove configuration)

SYM SS916-G3H6 White w/ Black grooves (3” x 6 sides hexagon groove configuration)

SYM SS105-G3HG Black w/ White grooves (3” x 6 sides hexagon groove configuration)

SYM SS100-G33DMD White (3” x 3” diamond groove configuration)

SYM SS916-G33DMD White w/ Black grooves (3” x 3” diamond groove configuration)

SYM SS105-G33DMD Black w/ White grooves (3” x 3” diamond groove configuration)

SYM SS100-G6CHEV3 White (6” x 3” chevron groove configuration)

SYM SS916-G6CHEV3 White w/ Black grooves (6” x 3” chevron groove configuration)

SYM SS105-G6CHEV3 Black w/ White grooves (6” x 3” chevron groove configuration)

Marlite Classic Symmetrix FRP Panels with Sani-coat Sealer are available in a variety of colors, pattern designs, graphics and images and scoring configurations, including:

SYM C100-G63 White (6” x 3” subway groove configuration)

SYM A916-G63 White w/ Black grooves (6” x 3” subway groove configuration)

SYM C105-G63 Black w/ White grooves (6” x 3” subway groove configuration)

SYM C100-G44 White (4” x 4” square groove configuration)

SYM C100-G66 White (6” x 6” square groove configuration)

SYM C105-G44 Black (4” x 4” square groove configuration)

SYM C140-G44 Ivory (4” x 4” square groove configuration)

SYM C145-G44 Silver (4” x 4” square groove configuration)

Specifier Note: Marlite Symmetrix SmartSeam FRP Panels require no division molding.  Marlite Classic Symmetrix FRP Panels require division molding.

Marlite Symmetrix FRP Panels are available in custom solid colors.

Specifier Note:  Retain and edit the following paragraph when finish solid color coating will be selected from the manufacturer’s or Sherwin-Williams color options.  Visit the Marlite website at www.marlite.com for color charts and sourcing information.

Solid Color Symmetrix FRP Panel: SYM C [_____] solid color name – groove configuration

Solid Color Symmetrix SmartSeam FRP Panel:  SYM SS [______] – solid color name – groove configuration

Marlite Symmetrix FRP Panels are available in custom digitally printed finishes featuring the BlueSky Advanced Finishing System.

Specifier Note:  Retain and edit the following paragraph when finish is selected from Marlite’s BlueSky gallery or custom print.  Visit the Marlite website at www.marlite.com for gallery color and pattern detail.

Gallery pattern:

            - Marble and granite

            - Brick and stone

            - Wood

            - Tile and mosaic

            - Cement

            - Metal

            - Textile

            - Leather

            - Aged wood and lap siding

            - Organic materials

            - Objects

            - Vector graphics

            - SYM C [_______]-SKY G[__] digital finish name – groove configuration

            - SYM SS [_______]-SKY G[__] digital finish name – groove configuration

Marlite Symmetrix FRP Panels are available in custom graphics and photographic images featuring the BlueSky Advanced Finishing System.

Specifier Note:  Retain and edit the following paragraph when finish incorporates custom scanned or uploaded image supplied by the Architect.  Visit the Marlite website at www.marlite.com for instructions and parameters regarding scanning services and upload process.

Custom Graphic: [Upload to manufacturer’s website] [scanned] image file as selected by the Architect.

Customer scan or supplied artwork, in a digital file format compatible with Marlite’s requirements and in a layout compatible with the panel dimensions as required for the installation.  Samples and/or revisions by Marlite Graphics Services to customer supplied artwork are to be submitted for customer approval.

        - Surface: Symmetrix FRP Panels are a smooth surface texture.

        - Fire Rating:  Class B (II) & Class C (III) Fire Rating.

        - Size: [Specifier to choose, or as indicated on drawings.] standard sizes are;

          - Marlite Symmetrix FRP

            - 48” x 96” [1.2m x 2.4m] x .090” (3mm) nom.

            - 48” x 108” [1.2m x 2.7m] x .090” (3mm) nom.

            - 48” x 120” [1.2m x 3m] x .090” (3mm) nom.

            - 48” x 48” ([1.2m x 1.2m] x .090” (3mm) nom.

Delete the following if resilient or contractor supplied bases are used.

BASE

Marlite Base Molding for 0.090” (2.29mm) thick FRP Panels

Color: [Black] [Quarry Red].

Profiles:

M 612 FRP Base Molding, 10’ length

M 651 Inside Corner

M 660 Outside Corner

M 620 LH End Cap

M 625 RH End Cap

TRIM MOLDING

The following are extruded PVC trim profiles. PVC colors are also available to coordinate with Sani-Coat colorways.  See current Marlite Finish Guide for available choice.

PVC Trim:  Thin-wall semi-rigid extruded PVC.

M 350 Inside Corner, [8’ length][10’ length]

M 360 Outside Corner, [8’ length][10’ length]

M 365 Division, [8’ length][10’ length]

Not Required with SmartSeam Panels

M 370 Edge, [8’ length][10’ length]

V 177 135° Inside Corner [8’ length] [White only]

V 179 135° Outside Corner [8’ length] [White only]

Color: [White][Ivory][Silver][Black][extruded custom harmonizing color]

The following are dual-durometer extruded polypropylene trim profiles with Marlite’s exclusive Dual-Seal Technology, designed to restrict the growth and propagation of harmful pathogens. Standard colorways are extruded with color throughout the profile.

Outside Corner Guard:

F 560SS Stainless Corner Guard, [8’ length] [10’ length]

Finish:  #4 brushed satin

M 961 PVC Outside Corner Guard

Color: [White, [8’ length][10’ length]][Natural Almond, [8’ length][10’ length]][Ivory, 10’ length][Silver, 10’ length][Light Grey, 10’ length]

ACCESSORIES

Specify rivets for use in areas with dramatic changes in temperature and/or humidity, where the substrate is unusually uneven, and in all low temperatures or cold storage applications.

Adhesive:  Either of the following construction adhesives complying with ASTM C 557.

Marlite C-551 FRP Adhesive - Water- resistant, non-flammable adhesive. [3.5 gallon can]

Titebond Advanced Polymer Panel Adhesive – VOC compliant, non-flammable, environmentally safe adhesive. [3.5 gallon can]

Marlite C-109 Low VOC Cartridge Adhesive required for interlocking SmartSeam Panels. [28 ounce cartridge]

Sealant:

Marlite Brand MS-250 Clear Silicone Sealant.

Marlite Brand MS-251 White Silicone Sealant.

For Seam joint application.

Marlite Brand - Color Match Sealant.

For Seam joint application.

EXECUTION

PREPARATION

Examine sub wall to determine that corners are plumb and straight, surfaces are smooth, uniform, clean and free from foreign matter, nails countersunk, joints and cracks filled flush and smooth with the adjoining surface.

Verify that stud spacing does not exceed 24” (61cm) on-center.

Repair defects prior to installation.

Level wall surfaces to panel manufacturer’s requirements.  Remove protrusions and fill indentations.

INSTALLATION

Comply with manufacturer's recommended procedures and installation sequence.

Cut panels to meet supports allowing 1/8” (3 mm) clearance for every 8 foot (2.4m) of panel.

Cut and drill with carbide tipped saw blades or drill bits, or cut with shears.

Apply panels to board substrate, above base, vertically oriented with seams plumb and pattern aligned with adjoining panels.

Install panels with manufacturer's recommended gap for panel field and corner joints.

Adhesive trowel and application method to conform to adhesive manufacturer’s recommendations.

For interlocking SmartSeam Panels (non-continuous vertical joints, i.e. subway groove configuration), apply Marlite C-109 Low VOC Cartridge adhesive using swirl technique at jagged panel edges.

Apply panel moldings to all panel edges using silicone sealant providing for required clearances.

All moldings must provide for a minimum 1/8” (3mm) of panel expansion at joints and edges, to insure proper installation.

Apply sealant to all moldings, channels and joints between the system and different materials to assure watertight installation.

CLEANING

Remove excess sealant from panels and moldings.  Wipe panel down using a damp cloth and mild soap solution or cleaner.

Refer to manufacturer's specific cleaning recommendations Do not use abrasive cleaners.

END OF SECTION 09 7720